## Slide 1: Weekly Meeting
2/10/2022
Mingyi Zhang

## Slide 2
2.5 cm
Light intensity 6 mW/cm2
29.4 mW
photons
57.3339 umol H2
At 380 nm
Will repeat this under 365 nm, 370 nm, 400 nm
Chart: Hydrogen production
| Category 1
STO 2 | 1.5607
BTO 2 | 57.3339
57.3339 umol
1.5607 umol
need to measure it again
I’m afraid the STO result is odd, but BTO makes sense to me.
20 mg powder in 20 ml water.
Run in Ar.
Unfortunately, they can’t quantify O2 because they didn’t calibrate the GC for O2.

## Slide 3
0% Al
1% Al
2% Al
3% Al
4% Al
5% Al
methanol
pH 2
pH 7
pH 12
methanol
pH 2
pH 7
pH 12
BTO + Al2O3 +SrCl2 in Al crucible
380 nm
16 h
10 mg in 0.4 ml solution
As the amount of Al increases, particle shape become irregular, and they don’t coarsen.

## Slide 4
BTO + Al2O3 +SrCl2 in Al crucible
400 nm
16 h
methanol
pH 2
pH 7
pH 12
methanol
pH 2
pH 7
pH 12
0% Al
2% Al
4% Al
1% Al
3% Al
5% Al

## Slide 5
BTO-sA-0%Al
BTO-sA-1%Al
BTO-sA-2%Al
BTO-sA-3%Al
BTO-sA-4%Al
BTO-sA-5%Al

## Slide 6
Al addition | Lattice parameter | Volume
0%Al | 3.9048(2) | 59.54
1%Al | 3.9059(9) | 59.59
2%AL | 3.9067(6) | 59.62
3%Al | 3.9063(1) | 59.61
4%Al | 3.9049(3) | 59.54
6%Al | 3.9041(5) | 59.51
BTO+Al+SrCl2 in Al crucible

## Slide 7
In Al crucible
In Pt crucible
Comparing the results in different types of crucibles
BTO + SrCl2 + Al2O3

## Slide 8
BTO-sP-0%Al
BTO-sP-1%Al
BTO-sP-2%Al
BTO-sP-3%Al
BTO-sP-4%Al
BTO-sP-5%Al

## Slide 9
Al addition | Lattice parameter | Volume
0%Al | 3.9056(1) | 59.57
1%Al | 3.9056(1) | 59.57
2%AL | 3.9070(3) | 59.64
3%Al | 3.9069(2) | 59.63
4%Al | 3.906(1) | 59.6
6%Al | 3.9066(8) | 59.62
BTO+Al+SrCl2 in Pt crucible

## Slide 10
Element | Weight % | Atomic % | Net Int. | Error %
O K | 44.05 | 58.77 | 203.94 | 10.21
MgK | 37.71 | 33.11 | 810.58 | 7.78
TiK | 18.24 | 8.13 | 642.63 | 1.81
Why it restructures to spinel?

## Slide 11
Element | Weight % | Atomic % | Net Int. | Error %
O K | 39.21 | 55.44 | 114.25 | 11.08
MgK | 34.59 | 32.18 | 560.34 | 8.22
TiK | 26.20 | 12.37 | 740.02 | 1.72

## Slide 12
I think this SBTO solid solution.
Only a small amount of Sr was replaced by Ba.

## Slide 13
It will form CTO.
But CaCl2 also reacts with Al2O3 and calcium aluminate
is insoluble.