## Slide 1: Weekly Meeting
9/11/2020
Mingyi Zhang

## Slide 2
Al 1%
Al 2%
Methanol
Methanol
pH 7
pH 7
pH 7
pH 7
pH 7
pH 7
Batch 1
Batch 2
Batch 3
Batch 4
Batch 5
Batch 6
Batch 7
All coated with
0.1wt% Rh and Cr (metal)

## Slide 3
Heat Stage
stirring
50mg powder + 0.5 ml solution
Methanol
Methanol
pH 7
pH 7
pH 7
pH 7
pH 7
pH 7
Al 1%
Al 2%
Batch 1
Batch 2

## Slide 4
Heat Stage
stirring
50mg powder + 0.5 ml solution + 1.5ml DI water
Methanol
Methanol
pH 7
pH 7
pH 7
pH 7
pH 7
pH 7
Al 1%
Al 2%
Batch 3
Batch 4

## Slide 5
Heat Stage
stirring
50mg powder + 0.5 ml solution (no water bath)
(~110 C)
Methanol
Methanol
pH 7
pH 7
pH 7
pH 7
pH 7
pH 7
Al 1%
Al 2%
Batch 5
Batch 6

## Slide 6
Heat Stage
50mg powder + 0.5 ml solution (no stirring)
Methanol
Methanol
pH 7
pH 7
pH 7
pH 7
pH 7
pH 7
Al 1%
Al 2%
Batch 7

## Slide 7
Dark to bright: 13nm
Dark to bright: 100nm
Evaporate a drop of Rh/Cr solution on a fresh
STO (100) single crystal
Then heat it at 350C for 1h.

## Slide 8
Based on my experiments in the past two months
Cocatalysts should be heated in a clean crucible (no Sr)
After Al salt treatment, water the powder more times to remove all SrCl2.
During the evaporation, weigh fewer samples every time and try to make it more uniform.
For a run with all pH data, it needs about 150mg STO powder. I could split the cocatalysts coating
process in 3 times (each for 50mg).