## Slide 1: Weekly Meeting
11/22/2019
Mingyi Zhang

## Slide 2
Al : STO
Method 1:
Mixing AlCl3 with SrCl2 (molar ration 1:100)
Method 2:
Heating undoped facet particles in Al flux
STO : Al2O3 : SrCl2 = 1 : 0.02 : 10
Heat at 1100C, 10h
Shape A
Shape B
Shape C
Shape D

## Slide 3
Shape A after treatment in Al flux (method 2)
From Domen’s paper.

## Slide 4
After Pt deposition

## Slide 5
After Mn deposition

## Slide 6
Shape B after treatment in Al flux (method 2)

## Slide 7
Shape B after treatment in Al flux (method 2)
Photo deposition of Pt

## Slide 8
Shape B after treatment in Al flux (method 2)
Photo deposition of Mn

## Slide 9
Shape C after treatment in Al flux (method 2)

## Slide 10
After Pt deposition

## Slide 11
Shape D after treatment in Al flux (method 2)

## Slide 12
After Pt deposition

## Slide 13
Shape C prepared with mothed 1

## Slide 14
Shape C prepared with mothed 1
Photo deposition of Pt

## Slide 15
Shape D prepared with mothed 1

## Slide 16
Photo deposition of Pt
Shape D prepared with mothed 1

## Slide 17
Hg lamp in our lab: a broad spectrum from 300nm to 800nm,
there is a sharp peak at 240 nm before the intensity goes to zero.
UV LED in photoreactor: 380nm ±15nm (365nm – 395nm)
380nm corresponds to 3.25eV
Indirect Band gap of STO: 3.25eV
Direct band gap: 3.75eV (330nm)
Is this LED enough to excite STO?