## Slide 1
1st
2nd
0 h
6 h
15.1 h

## Slide 2
S09, 2 | S19, 2 | S29, 2 | S39, 2 | S010, 2 | S110, 2 | S210, 2 | S310, 2 | S011, 2 | S111, 2 | S211, 2 | S311, 2
S09, 6 | S19, 6 | S29, 6 | S39, 6 | S010, 6 | S110, 6 | S210, 6 | S310, 6 | S011, 6 | S111, 6 | S211, 6 | S311, 6
S09, 12 | S19, 12 | S29, 12 | S39, 12 | S010, 12 | S110, 12 | S210, 12 | S310, 12 | S011, 12 | S111, 12 | S211, 12 | S311, 12
K09, 2 | K19, 2 | K29, 2 | K39, 2 | K010, 2 | K110, 2 | K210, 2 | K310, 2 | K011, 2 | K111, 2 | K211, 2 | K311, 2
K09, 6 | K19, 6 | K29, 6 | K39, 6 | K010, 6 | K110, 6 | K210, 6 | K310, 6 | K011, 6 | K111, 6 | K211, 6 | K311, 6
K09, 12 | K19, 12 | K29, 12 | K39, 12 | K010, 12 | K110, 12 | K210, 12 | K310, 12 | K011, 12 | K111, 12 | K211, 12 | K311, 12
K211P, 2 | K211P, 6 | K211P, 12 | S211, 6 | K211M, 2 | K211M, 6 | K211M, 12 | S211, 6 | None, 2 | None, 6 | None, 12 | S211, 6
S211, 324, 6 | S211, 164, 6 | S211, 84, 6 | S211, 44, 6 | S211, 6 | S211, 648, 6 | S211, 328, 6 | S211, 168, 6 | S211, 88, 6 |  |  | 
S09,2
S: SrCl2 flux (K for KCl flux)
0: molar ratio Al2O3: SrTiO3 =0%
9: 900 °C flux treatment
2: pH 2
General condition:
6.4 mg powder coated with RhCrOx, 0.4 ml DI water
Except:
P: Pt 1 wt% coating
M: 8 vol% methanol
middle term: 3.2, 1.6, 0.8, 0.4 mg powder in 0.4 ml water; 6.4, 3.2, 1.6, 0.8 mg powder in 0.8 ml water

## Slide 3
0
6
Hydrogen production (𝝻mol) vs Reaction time (h)
28.6
0
1st 6h

## Slide 4
0
6
Hydrogen production (𝝻mol) vs Reaction time (h)
28.6
0
2nd 6h

## Slide 5
0
15
Hydrogen production (𝝻mol) vs Reaction time (h)
28.6
0
2nd 15.1 h

## Slide 6
The observable maximum rate:
Fit the data above the lowest calibrated limit;
Get the intersection of the log function and the lowest calibrated limit;
Calculate the rate at this point.
Slope
The calibrated limit

## Slide 7
1st #18
1st #19
1st #80
1st #84
2nd #18
2nd #19

## Slide 8
2nd #80
2nd #84
2nd #19
2nd #80
2nd #84
2nd #18

## Slide 9
Calibrated H2 range: 5 to 50 vol%
2.86 to 28.6 𝝻mol
BL: Below Limit
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h

## Slide 11
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21%
(SrCl2 flux, molar ratio Al2O3: SrTiO3 =2%, 1100 °C flux treatment, pH 2)

## Slide 12
Some organics might be mixed into the powder of S111, S211, S311 during the coating of RhCrOx

## Slide 13
Sample | Hydrogen generation rate, µmol/h/100mg | BET surface area, m2/g | 2[Al]/([Sr]+[Ti]), %
STO (pristine) | 1 | 3.6 | 0.04
STO (flux-Y) | 3 | 1.5 | 0.02
STO (flux-Al), 1100 °C | 550 | 0.9 | 0.31
STO (flux-Al), 1000 °C | 500 | 1.3 | 0.11
STO (flux-Al), 900 °C | 20 | 1.9 | 0.12
10%Al-STO (flux-Y) | 700 | 2.4 | 1.36
1%Al-STO (flux-Y) | 400 | 2.7 | 1.01
0.1%Al-STO (flux-Y) | 20 | 0.9 | 0.12
0.1%Al-STO (ssr-Y) | 150 | 1.7 | 0.1
1%Al-STO (ssr-Y) | 80 | 3.0 | 1.07
5%Al-STO (ssr-Y) | 50 | 3.7 | 4.24
10%Al-STO (ssr-Y) | 30 | 3.9 | 8.25
4%Al-STO (flux-Al) | 80 µmol/h/20mg =4000 µmol/h/g |  | 
1100 °C, 10 h
1150 °C, 10 h
https://pubs.rsc.org/en/content/articlehtml/2015/ta/c5ta04843e

## Slide 14
https://pubs.acs.org/doi/abs/10.1021/acs.chemmater.6b02907
 | Domen’s | Ours
µmol/h | 80 | 4.48
mg | 20 | 6.4
µmol/h/g | 4000 | 700

## Slide 15
Surface area: TiO2 coating
Same sol-gel method, 500/600/700 °C annealing
Whether the dopant can be kept
Sample | Annealing temperature, °C | BET surface area, m2/g
STO/TiO2 | 500 | 47
 | 600 | 41
 | 700 | 22
PTO/TiO2 | 400 | 117
 | 500 | 74
 | 600 | 26
https://www.sciencedirect.com/science/article/pii/S2542435117302246

## Slide 16
Reaction conditions comparison
 | Domen’s 0.4% STH | Ours
Powder loading | 20 mg/20 ml=1 mg/ml | 6.4 mg/0.4 ml=16 mg/ml
Light source | AM 1.5 G solar simulator | 2 100 W UV LED (380 nm)

## Slide 17
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
pH | S09 | S19 | S29 | S39 | S010 | S110 | S210 | S310 | S011 | S111 | S211 | S311
2 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
6 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
12 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21%
pH effect: pH 6 is better than 2 or 12

## Slide 18
 | PZC
TiO2 | 6
BaTiO3 | 6.5
SrTiO3 | 8.5
pH effect: pH 6 is better than 2 or 12

## Slide 19
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
salt | 09 | 19 | 29 | 39 | 010 | 110 | 210 | 310 | 011 | 111 | 211 | 311
SrCl2 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
SrCl2 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
SrCl2 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
KCl | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
KCl | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
KCl | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21%
Salt: SrCl2 better than KCl

## Slide 20
https://pubs.rsc.org/en/content/articlehtml/2013/cy/c3cy00014a
KCl
SrCl2
Salt: SrCl2 better than KCl
Li’s and mine SrTiO3 core: flux treatment with KCl at 1100 °C for 5 h: poor performance.
This Al:SrTiO3: 1100 °C for 10 h.
flux treatment with at 1000 °C for 5 h.
BaTiO3

## Slide 21
2 µm
0% Al
2% Al
1% Al
3% Al
900 °C
1000 °C
1100 °C
SrTiO3+Al2O3+KCl

## Slide 22
2 µm
0% Al
2% Al
1% Al
3% Al
900 °C
1000 °C
1100 °C
SrTiO3+Al2O3+SrCl2

## Slide 23
K211
S211

## Slide 24
Ion | Ionic radius, pm
Al3+ | 67.5
Ti4+ | 74.5
K+ | 152
Sr2+ | 132
Salt | Melting point, °C | Boiling point, °C
KCl | 770 | 1420
SrCl2 | 874 | 1250
K doping might have affected the crystallization: XPS, XRD

## Slide 25
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
pH | S09 | S19 | S29 | S39 | S010 | S110 | S210 | S310 | S011 | S111 | S211 | S311
2 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
6 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
12 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21%
Annealing temperature: 1000 °C/1100 °C best

## Slide 26
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
pH | S09 | S19 | S29 | S39 | S010 | S110 | S210 | S310 | S011 | S111 | S211 | S311
2 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
6 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
12 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21%
Doping concentration: molar ratio Al2O3: SrTiO3 =2% or 3% (surface area)

## Slide 27
Calibrated H2 range: 5 to 50 vol%
2.86 to 28.6 𝝻mol
BL: Below Limit
(<148 𝝻mol/(g h))
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 294 | BL
 | BL | BL | 107 | 784 | BL | 620 | 873 | 709 | BL | BL | 738 | 846
 | BL | BL | BL | 289 | BL | BL | 458 | 121 | BL | BL | 528 | 859
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 615 | BL | BL | BL | 645 | BL | BL | BL | 927
 | 1726 | BL | BL | BL | 550 | 212 | 512 | 665 | BL |  |  | 
1st 6h
Domen’s: pH or TiO2 coating ; Try platinization/methanol on other powders

## Slide 28
The potential of TiO2 coating
2 µm
Sample | BET surface area, m2/g | Hydrogen generation rate, µmol/g/h
STO/TiO2 600 °C | 41 | 212
BTO core | 0.8 | 0
STO core | 1 | 0.5

## Slide 29
PTO:Al2O3:PbCl2 (molar ratio) | Annealing temperature (°C) | Salt | Cocatalyst | Scavenger
1:0:10 | 600/700/800 | PbCl2 | Rh 0.1wt%, Cr 0.1 wt% | None
1:0.01:10 | 800/900/1000 | KCl |  | 
1:0.02:10 |  |  |  | 
1:0.03:10 |  |  |  | 
Try Al doped PbTiO3
Salt | Melting point, °C | Boiling point, °C
KCl | 770 | 1420
SrCl2 | 874 | 1250
PbCl2 | 501 | 950

## Slide 30
Powder (mg) | 3.2 | 6.4 | 6.4 | 3.2 | 1.6
Solution (ml) | 0.4 | 0.4 | 0.8 | 0.8 | 0.8
Powder/Solution (mg/ml) | 8 | 16 | 8 | 4 | 2
Mass specific rate (µmol/h/g) | 1726 | 695 | 212 | 512 | 665
Rate (µmol/h) | 5.52 | 4.45 | 1.36 | 1.64 | 1.06
1st 6h
3.2 mg/ 0.4 ml

## Slide 31
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | 263 | 775 | BL | 745 | 930 | 828 | BL | BL | 969 | 995
 | BL | BL | BL | BL | BL | 287 | 397 | 376 | BL | BL | 688 | 827
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 770 | BL | BL | BL | 874 | BL | BL | BL | 1295
 | 2133 | BL | BL | BL | 809 | 286 | 711 | 1243 | BL | BL | BL | BL
2nd 6h
Effect of salt, annealing temperature, doping concentration, and pH all similar to the 1st run.
Average value ± Standard deviation: 943 ± 211 𝝻mol/(g h) ~22%
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21% (1st run)

## Slide 32
Powder (mg) | 3.2 | 6.4 | 6.4 | 3.2 | 1.6
Solution (ml) | 0.4 | 0.4 | 0.8 | 0.8 | 0.8
Powder/Solution (mg/ml) | 8 | 16 | 8 | 4 | 2
Mass specific rate (µmol/h/g) | 2133 | 943 | 286 | 711 | 1243
Rate (µmol/h) | 6.83 | 6.04 | 1.83 | 2.27 | 1.99
2nd 6h
3.2 mg/ 0.4 ml

## Slide 33
Hydrogen generation rate, 𝝻mol/(g h) |  |  |  |  |  |  |  |  |  |  |  | 
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | 74 | BL
 | BL | 370 | 318 | 679 | BL | 671 | 834 | 740 | 286 | BL | 877 | 886
 | BL | BL | BL | 119 | BL | 322 | 364 | 376 | BL | 317 | 602 | 751
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL | BL
 | BL | BL | BL | 707 | BL | BL | BL | 838 | BL | BL | BL | 1210
 | 1896 | 729 | 1214 | BL | 750 | 260 | 682 | 1111 | 676 | BL | BL | BL
2nd 15 h
Effect of salt, annealing temperature, doping concentration, and pH all similar to the 1st run.
Average value ± Standard deviation: 876 ± 199 𝝻mol/(g h) ~23% (2nd run 15 h)
Average value ± Standard deviation: 943 ± 211 𝝻mol/(g h) ~22% (2nd run 6 h)
Average value ± Standard deviation: 695 ± 146 𝝻mol/(g h) ~21% (1st run)

## Slide 34
Powder (mg) | 3.2 | 1.6 | 0.8 | 6.4 | 6.4 | 3.2 | 1.6 | 0.8
Solution (ml) | 0.4 | 0.4 | 0.4 | 0.4 | 0.8 | 0.8 | 0.8 | 0.8
Powder/Solution (mg/ml) | 8 | 4 | 2 | 16 | 8 | 4 | 2 | 1
Mass specific rate (µmol/h/g) | 1896 | 729 | 1214 | 876 | 260 | 682 | 1111 | 676
Rate (µmol/h) | 6.07 | 1.17 | 0.97 | 5.61 | 1.66 | 2.18 | 1.78 | 0.54
2nd 15 h
3.2 mg/ 0.4 ml
pipette/tips