## Slide 1: Weekly Meeting
8/12/2021
Mingyi Zhang

## Slide 2
1100 C
10h
2g SrCl2
It is clean inside but a lot of stuff outside.

## Slide 3
Chart: After treatment
Chart: Before treatment
SrO
SrCO3
Sr(OH)2
In Al crucible
No longer SrCl2
SrCl2

## Slide 4
1100 C
10h
1g SrCl2

## Slide 5
Chart: After heatment in pt crucible
Chart: Before treatment
SrCl2
Mostly SrCl2
and some Sr(OH)2?
SrO
SrCO3
Sr(OH)2

## Slide 6
10h
2h
1h
5h
Treated in flux
for different time
in Pt crucible
1% Al

## Slide 7
10 h
5 h
2 h
1 h

## Slide 8
Heated in flux for 5h in Pt crucible
Steps?

## Slide 9
Annealed in O2 overnight
400C
Flux treated for 10h
Flux treated for 10h
Flux treated for 5h
Flux treated for 5h
These two samples are
from a different batch in
another furnace
Color did not
change obviously after O2 anneal

## Slide 10
Not annealed in O2
Annealed in O2
Treated in flux for
10 h
5 h
2 h
1 h
methanol
pH 3
pH 7
pH 12
methanol
pH 3
pH 7
pH 12
1% Al doped during hydrothermal synthesis
These two samples are from a different batch in another furnace.